## Slide 1
Indian Institute of Technology Guwahati Research & Industrial Conclave 2025
—Electrically Tunable Selective Light Absorber using Epsilon-Near-Zero InSb and High-k Dielectrics —
RIC ID: RICf6219bdb
Soham Chatterjee1, Rajib Lochan Ghadei2, Rishi Maiti3
1,2,3 Department of Physics
Indian Institute of Technology Guwahati, Guwahati-781039, India
Presented at:
2025 Research & Industrial Conclave (RIC 2025)
Indian Institute of Technology Guwahati, Assam, India, 10 -12 October 2025

## Slide 2: Motivation & Background
Problem? Static optical components limit adaptability in modern photonic systems.
Solution? Electrically tunable elements enable real time control of optical properties.
How? Epsilon-Near-Zero (ENZ) materials allow strong modulation when Re(ε) → 0.
2
Optical Color Filter
White light
Light of selective wavelength absorbed
Switch currently off
Optical Color Filter
White light
Light of different wavelength selectively absorbed
Switch on

## Slide 3: Objective
Design and simulate an electrically tunable selective light absorber based on n-InSb.
Compare high-k dielectrics (TiO₂, HfO₂, ZrO₂) to find optimal tunability and best absorption characteristics.
Show that on altering cavity thickness, resonant wavelength shifts from Visible to near IR range.
Demonstrate bias-dependent ENZ shift and spectrally selective absorption.
3

## Slide 4: Device Architecture
4
Why n-InSb as ENZ?
high electron mobility
narrow bandgap
CMOS compatible
ideal for visible/IR modulation.
Active layer (ENZ+insulator) thickness and the choice of insulator determines the resonant wavelength
Electrical gating: 0 V and 15 V
Fig 1. Schematic

## Slide 5: Simulation and Computational Details
5
Ansys Charge;
Electrostatic Simulations
Drude Model;
Compute R.I of ENZ material
Transfer Matrix Method;
Compute Reflectance Spectra
Optical data for materials were obtained from Palik
Electrical properties from Ansys Charge Materials library
Constant Dopant value of 3.5×10¹⁷ cm⁻³ was applied to InSb layer

## Slide 6: Theory
Electrostatic Calculations:
6
Drude Dispersion Model:
Transfer Matrix Method :
Where Mij are elements of the Overall Transfer Matrix

## Slide 7: Electrostatic Simulation Results
7
Carrier Concentration profile across InSb on 15V biasing
15 V bias increases electron density: 3.5×10¹⁷ → 2.68×10²² cm⁻³
Strong carrier accumulation near the semiconductor–insulator interface
ON 15V BIASING

## Slide 8: Electrostatic Simulation Results
8
Electrical Potential Distribution (V) for Active layer (ENZ+insulator) on 15V biasing
A fraction of the total external voltage suffers a drop across the semiconductor layer.
ON 15V BIASING
InSb-Metal interface

## Slide 9: Drude Modelling Results for InSb
9
(a) Permittivity plot (b) Refractive Index plot for n-InSb
With application of voltage bias, there is a shift of ENZ wavelength from 35.17 microns to 126 nm.
where N1 = 3.5 × 10^17 cm−3 and N2 = 2.68 ×10^22 cm−3.

## Slide 10: Optical Results — Visible Range
10
HfO₂
ZrO₂
TiO₂

## Slide 11: Result Comparison among Dielectrics
11
Insulator used in the device | Resonant Wavelength On 0V biasing | Resonant Wavelength On 15V biasing | Spectral Shift (Blue Shift) | Reflectance dip at 0V biasing | Reflectance Dip at 15V biasing
HfO₂ | 520 nm | 480 nm | 40 nm | ~95.3% | ~97.6%
TiO₂ | 495 nm | 460 nm | 35 nm | ~95% | ~97%
ZrO₂ | 505 nm | 470 nm | 35 nm | ~95% | ~97%

## Slide 12: Optical Results — Near IR Range (Thicker Cavity)
12
Cavity thickness engineered such that semiconductor: 50 nm, insulator: 100 nm
HfO₂
TiO₂
ZrO₂

## Slide 13: Result Comparison among Dielectrics (Thicker Cavity)
13
Insulator used in the device | Resonant Wavelength On 0V biasing | Resonant Wavelength On 15V biasing | Spectral Shift (Blue Shift)
HfO₂ | 1.10 microns | 895 nm | 115 nm
TiO₂ | 1.19 microns | 1.09 microns | 100 nm
ZrO₂ | 1.13 microns | 1.025 microns | 105 nm
Reflectance dip falls to 73.7% approximately.

## Slide 14: Optical Results — Incident Angle Colormap
14
TE and TM polarized colormaps for Device with ZrO₂ as insulator

## Slide 15: Optical Results – Polar Plot
15
TE and TM polarization analyzed using TMM.
TE mode: nearly angle-independent reflectance.
TM mode: shows pseudo-Brewster angle with sharp reflectance minimum.
Reflectance Polar Plots for TE and TM polarized modes with ZrO₂ chosen as insulator for the Device
--
--
--

## Slide 16: Conclusion
16
Electrically tunable ENZ-InSb light absorber successfully demonstrated.
Best case achieved tunability:
40 nm (visible)
115 nm (near-IR)
The optimum tunability and absorption peak was obtained when Hafnium Oxide was chosen as the dielectric for our device architecture
Compact and CMOS-compatible design.

## Slide 17
17
THANK YOU
I WOULD BE HAPPY TO TAKE ANY QUESTIONS….
Speaker and First Author: Soham Chatterjee
Affiliation: B.Tech Engineering Physics, IIT Guwahati (2023-2027) Email: chsoham04@gmail.com